Project #2: Automation of Concrete Mix Design

# CIVE 202 -001

# Written Summary

Date Submitted for Review February 24, 2026

Camdin Wagner McGuigan

Michael McCarthy

Eddie Vargas

Table of Contents

Table of Figures	2

Written Summary	3

Introduction:	3

Results:	4

Scenario #1	4

Scenario #2	5

Scenario #3	6

Scenario #4	7

References:	8

# Table of Figures

Figure 1- 47B-3500 Final Mix Design	4

Figure 2- RES2023 Final Mix Design	5

Figure 3- 504-705	6

Figure 4- SF-3,625 NDOT Final Mix Design	7

# Written Summary

## Introduction:

Our group was assigned to automate the Nebraska Department of Transportation (NDOT) concrete mix design model by converting the existing Excel-based workflow into a structured Python program. The original NDOT Mix Design worksheet requires users to manually input material properties and design parameters to calculate the required material weights for one cubic yard of concrete. Although the Excel model performs the necessary engineering calculations, it depends on spreadsheet logic and manual interaction, which can limit transparency and repeatability. The purpose of this project was to translate that logic into clearly defined Python functions to create a more organized, reliable, and reproducible computational tool.

The objective of the automation was to replicate the Excel calculations using Python functions and sequential user input prompts that guide the user through the mix design process. The program collects required inputs, performs the necessary calculations, and generates a formatted weight chart for one cubic yard of concrete. In addition, four realistic concrete mix design scenarios were researched and evaluated using the automated model to verify functionality and compare how changes in input parameters affect final material quantities. This report outlines the translation process, identifies the required inputs and outputs, and presents a comparison of the four evaluated concrete mix designs.

## Results:

## Scenario #1

The first scenario used in testing the automated concrete design is (47B-3500), which is found in the NDOT Pavement Design Manual under 1002.02 General Specifications. This specific mix design is used for structural concrete and paving because of its high strength. The inputs of this concrete mix design were valued at: cement = 600lbs, fly ash = 141lbs, silica fume= 0, other scm= 0, water to cement ratio= .45, air content= 6.5, fine aggregate= 30%, coarse aggregate= 70%, other aggregate= 0%, sg (specific gravity) cement=3.15, sg fly ash= 2.30, sg silica fume= 2.20, sg other scm= 2.65, sg fine aggregate= 2.60, sg coarse aggregate= 2.65, sg other aggregate= 2.65. By putting these inputs into the code, the following table was created with reference, scenario, and data displayed in an organized, formatted table (Figure 1).

Figure 1- 47B-3500 Final Mix Design

## Scenario #2

The second iteration to test the code base involved using a concrete mix design for the Tennessee Department of Transportation (TDOT) that consisted of a mixture of Limestone and Manufactured sand. This mixture, classified by TDOT as A-LS1-MS-0, is a Class A concrete used mainly for transportation infrastructure due to its high strength and durability (Saykat et al., 2025). The inputs for this design were cement: 423 lbs., Fly Ash: 141, Target Water/Cement Ratio: 0.45, Target Air Content: 6.0%, Fine Aggregate: 42%, Coarse Aggregate: 35%, Other Aggregate: 23%, Cement special gravity: 3.15, Fly Ash specific gravity: 2.3, Fine Aggregate specific gravity: 2.75, Coarse Aggregate specific gravity: 2.75, Other Aggregate specific gravity: 2.62. When these inputs were used to validate the code, a table was displayed specifying the target weights required for each material to produce one cubic yard of A-LS1-MS-0 (Figure 2).

Figure 2- RES2023 Final Mix Design

## Scenario #3

Figure 3- 504-705

The figure shows the Scenario 3 that I got from the Nevada Department of Transportation (NDOT). The scenario 3 has a (504-705) using the Class of Concrete (A and AA). The inputs for the Nevada Department of Transportation use for Cementitious Materials (A-D), cement :600 lbs., fly ash: 100lbs, silica: 0, other SCM: 0, for Design Parameters (E-F) water cement ratio: 0.45, air content: 6%, Aggregate Percentages (G-I) fine aggregate: 40%, coarse aggregate: 60%, other aggregate: 0, SCM Specific Gravities (J-M) gravity of cement: 3.15, gravity of fly ash: 2.30, gravity of silica: 2.20, gravity of other SCM: 2.60, Aggregate Specific Gravity (N-P) gravity of fine aggregate: 2.65, gravity of coarse aggregate: 2.70, gravity of other aggregate: 2.60. Using all this information correctly in the code you should get something like the figure show for the Scenario 3.

## Scenario #4

For the final iteration of testing the automated concrete mix design code base, a scenario involving the use of SF-3,625 from the NDOT Standard Specification for Portland Cement Concrete was used (Nebraska Department of Transportation, 2020). This mix design, differing from the others tested, does not have any Fly Ash but instead uses a mix of cement and silica fume to reduce permeability and increase strength earlier in the curing process. These advantages in the different proportions of materials make it suitable for use as a paving overlay on older slabs of paving. The inputs for this mix design are Cement: 565 lbs., Silica Fume 51 lbs., Water/Cement Ratio: 0.38, Air Content: 6.0%, Fine Aggregate: 50%, Coarse Aggregate: 50%, Specific gravity cement: 3.15, Specific gravity silica flume: 2.20, Specific gravity Fine Aggregate: 2.62, Specific gravity Coarse Aggregate: 2.65. The figure below details the target weights required for each material to produce one cubic yard of SF-3,625 per NDOT standard specification (Figure 4).

Figure 4- SF-3,625 NDOT Final Mix Design

## References:

Saykat, S., Napper, C., Abd-Elssamd, A., & Ma, Z. J. (2025). Optimized aggregate gradations for concrete mixture designs (Final Report No. RES2023-16). Tennessee Department of Transportation.

Nebraska Department of Transportation. (2020). Section 1002: Portland cement concrete (100.02) [Standard specification].

Nevada Department of Transportation (NDOT). (2014). Standard Specifications for Road and Bridge Construction, Section 501: Portland Cement Concrete.
 https://www.dot.nv.gov/home/showpublisheddocument/6916/636257041112930000

Nebraska Department of Transportation, Pavement Design Manual, Nebraska Dept. of Transportation, Lincoln, NE, https://dot.nebraska.gov/media/jjwpyezr/pavdesignmanual.pdf.